GALVANIC SERIES OF METALS AND ALLOYS

CORRODED END ( ANODIC OR LEAST NOBLE)

MAGNESIUM

●
MAGNESIUM ALLOYS

●
ZINC

●
ALUMINIUM 5052, 3004, 3003, 1100, 6053

●
CADMIUM

●
ALUMINIUM 2117, 2017, 2024

●
MILD STEEL (1018), WROUGHT IRON

●
CAST IRON, LOW ALLOY HIGH STRENGTH STEEL

●
CHROME IRON (ACTIVE)

●
STAINLESS STEEL, 430 SERIES (ACTIVE)

●
302, 303, 321, 347, 410,416, STAINLESS STEEL (ACTIVE)

●
316, 317, STAINLESS STEEL (ACTIVE)

●
ALUMINIUM BRONZE (CA 687)

●
LEAD - TIN SOLDERS

●
LEAD

●
TIN

●
NICKEL (ACTIVE)

●
BRASS

●
COPPER (CA102)

●
MANGANESE BRONZE (CA 675), TIN BRONZE (CA903, 905)

●
SILICONE BRONZE

●
NICKEL SILVER

●
COPPER - NICKEL ALLOY 90-10

●
COPPER - NICKEL ALLOY 80-20

●
430 STAINLESS STEEL

●
NICKEL, ALUMINIUM, BRONZE (CA 630, 632)

●
SILVER SOLDER

●
NICKEL (PASSIVE)

●
CHROME IRON (PASSIVE)

●
302, 303, 304, 321, 347, STAINLESS STEEL (PASSIVE)

●
316, 317, STAINLESS STEEL (PASSIVE)

●
IRON ALLOY (PASSIVE)

●
SILVER

●
TITANIUM

●
GRAPHITE

●
ZIRCONIUM

●
GOLD

●
PLATINUM

PROTECTED END (CATHODIC OR MOST NOBLE)